## Slide 1: SB Certification for Mixture-Based Specification for Flexible Base
Summary of Spec
Test Procedures
Actions to Take for Non-Compliance
October 31, 2012

## Slide 2: Purpose of ABQMS
Establish List of Qualified Producers
Producers Responsible for Process Control/Quality Control
Reduce TxDOT Sampling and Testing
Expedite Aggregate Base Acceptance
Share Responsibility (Producer/TxDOT) for Quality and Uniformity
Reduce Cost and Time for Process Control, QC/QA Sampling and Testing and Acceptance
Reduce Risk to Producer and TxDOT
Other

## Slide 3: Process
Full Approval
Conditional Approval
Reject
Reject with Request for Additional Information
TxDOT Review of Application
Approve
Producer Application for ABQMS

## Slide 4: Aggregate
Type
A – Crushed Stone
B – Crushed/Uncrushed Gravel
C – Crushed Gravel
D – Crushed Stone/Crushed Concrete
E – As Shown on Plans
Grade
Grades 1 to 5 (Table 1)
Test methods, responsibilities, and minimum classification levels on Handout
Notes: See Handouts for details on Aggregate and test methods employed, along with agency and contractor responsibilities

## Slide 5: TxDOT Verification Tests*
Test | Test Method | Initial Production Frequency, Tons | Normal Production Frequency, Tons | Loadout Frequency, Tons
Gradation | TEX-110-E | 3,000 | 10,000 | 10,000
Atterberg Limits | TEX-104-E TEX-106-E | 3,000 | 10,000 | 10,000
Wet Ball Mill | TEX-116-E | 3,000 | 10,000 | 10,000
Sulfate Content | TEX-145-E | 3,000 | 10,000 | 10,000
Compressive Strength | TEX-117-E | 3,000 | 10,000 | 10,000
* Tests Can Be Performed by TxDOT at Any Time |  |  |  | 

## Slide 6: Operational Tolerances Allowable Material Property (Production) Differences and Specification Limits
Property | Test Method | Allowable Difference from Current JMF Target | Allowable Difference between Contractor and Engineer Test Results | Specification Limits for Pay Factor Determination
Gradation Accumulative Percent Passing |  |  |  | 
2 ½ in | Tex-110-E |  |  | 
1 ¾ in |  | 5 | 5 | 
7/8 in |  | 5 | 5 | 
3/8 in |  | 5 | 5 | 
No. 4 |  | 5 | 5 | Plus or minus 5
No. 40 |  | 3 | 3 | 

## Slide 7: Operational Tolerances Allowable Material Property (Production) Differences and Specification Limits, (Cont’d)
Property | Test Method | Allowable Difference from Current JMF Target | Allowable Difference between Contractor and Engineer Test Results | Specification Limits for Pay Factor Determination
Liquid Limit | Tex-104-E | 5 | 5 | 
Plasticity Index | Tex-105-E Tex-106-E | 4 | 4 | 
Wet Ball Mill, Max | TEX-116-E | 5 | 5 | 
Wet Ball Mill, % Increase Passing the No. 40 Sieve Percentage Points |  | 4 | 4 | 

## Slide 8: Operational Tolerances Allowable Material Property (Production) Differences and Specification Limits, (Cont’d)
Property | Test Method | Allowable Difference from Current JMF Target | Allowable Difference between Contractor and Engineer Test Results | Specification Limits for Pay Factor Determination
Sulfate Content, ppm | Tex-145-E | 500 | 500 | 
Min. Compression Strength, psi | Tex-117-E |  |  | 
Lateral Pressure, 0 psi |  | 10 | 8 | 
Lateral Pressure, 3 psi |  | 15 | 12 | 
Lateral Pressure, 15 psi |  | 20 | 15 | 
Optimum Moisture Content, % | Tex-113-E | 0.3 | 0.3 | 
Max Dry Density, lb per cu. ft. |  | 1.0 | 1.0 | 

## Slide 9: Placement Acceptance
Lot Size
  4 Sublots per Lot
  Area Placed by 4,000 Tons
Pay Factor for Lot 1-1.00
Rework or Remove and Replace Any Sublot in Lot 1 with Relative In-place Density Less than 98%

## Slide 10: Placement Sampling
Random Sampling (Engineer)
Property | Samples per sublot | Samples per lot
In-place density | 4 | 
In-place moisture content | 4 | 
Thickness | 1 | 
Lab compacted moisture-density relationship |  | 1

## Slide 11: Placement Testing Placement Testing Frequency, Allowable Differences and Specification Limits)
Property | Test Method | Minimal Contractor Testing Frequency | Minimal Engineer Testing Frequency | Allowable Difference from Current JMF Target | Allowable Difference between Contractor and Engineer | Specification Limits
Optimum Moisture Content, % | Tex-113-E | 1 per lot | 1 per 3 lots | 0.3 (percentage points) | 0.3 (percentage points) | 
Maximum Dry Density, lb per cu. ft |  |  |  | 1.0 | 1.0 | 
In-place Density, % 1 | Tex-115-E | 4 per sublot | 1 per sublot |  | 2.0 (percentage points) | 100
In-place Moisture Content, % 1 |  |  |  |  | 0.5 (percentage points) | ± 1.5
Thickness, in. | Tex-140-E | 1 per sublot | 1 per sublot |  | 0.5 | – 0.5 + 0.5

## Slide 12: Operational Tolerance/ Suspend Placement
Property | Out of Operational Tolerance |  | Suspend Production | 
 | JMF | Specification | Parameter | No. of Consecutive Sublot/Lots
In-place density/ moisture content |  | X | In-place density or moisture content individually | 2
 |  |  | Either in-place density or moisture content | 3
Thickness |  | X | Thickness | 2
Lab Compacted moisture-density relationship | X |  | Moisture content or dry density individually | 2
 |  |  | Either moisture content or dry density | 3