TECHNICAL MEMORANDUM

Task Report   #2.2, Developing Very Thin Overlays with Locally Available Aggregates for    Each District

TxDOT Project 9-1529, Low Cost Safety Solutions, Pavement Preservation and Maintenance Practices for Rural Highways

DATE:	May 10, 2012

TO:	Kelli Williams, Project Director

Texas Department of Transportation

COPY TO:	Wade Odell, Research and Technology Implementation Office, TxDOT

Frank Espinosa, Research and Technology Implementation Office, TxDOT

Mary Levien, Research Development Office, TTI

Erlinda Olivarez, Research Development Office, TTI

FROM:	Lance Bullard, Research Supervisor

Cindy Estakhri, Research Engineer

Tom Scullion, Senior Research Engineer

Xiaodi Hu, Research Associate

Texas Transportation Institute

FOR MORE INFORMATION:

Name:	Tom Scullion – Texas Transportation Institute

Phone:	979-845-9910

Email:	t-scullion@tamu.edu

EXECUTIVE SUMMARY:

## The objective of this subtask was to generate crack resistant hot mix designs which could be placed very thin using locally available materials for each of the West Texas Districts wanting to participate in this study. Crack Attenuating Mixes (CAMs) had been placed in other parts of the state with good performance, though not in West Texas.  Local aggregates meeting minimum quality and gradation requirements were solicited from 10 districts.  Asphalt binders were also requested.

## TTI used a new design approach based on recent research where the performance tests (Hamburg and Overlay Test) were run first for a range of asphalt contents in an attempt to identify an acceptable window of binder contents where both cracking and rutting requirements are met. The volumetrics were then checked at the binder content at the middle of the acceptable range.

## In addition to the CAM mix designs, fine graded permeable friction course (PFC) and fine graded stone matrix asphalt (SMA) mixes were developed for two of the aggregate sources.  A summary of all the mix designs is presented in the following tables and a detailed discussion of all test results follows.  Spreadsheets for each mix design have been submitted separately as product P1 from this research study.

## A total of 6 mixes were selected for placement at the Pecos Test Track; two CAM’s, two PFC’s and two fine SMA’s. Based on the results presented in this report the locally available Hoban from Pecos and the Eastland aggregates from Abilene District were used in the construction of test sections.   These mix designs are shaded in blue in the following table.  These mixes were successfully placed on the track in 2011, and the construction details and performance histories will be described in subsequent technical memos.

Table A.  Summary of All Mix Designs Completed in Subtask 2.2. (Accompanying spreadsheets were submitted to TxDOT separately).

| Materials | Mix ID/Type | Combined Gradation | AC Content | Density | Hamburg Test | Overlay | Outcome | Remarks |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  | Cycles |  |  |
| Eastland | Mix 1 CAM | 38% Grade 6 + 33% Man Sand + 28% Scng + 1% lime | 6.4% (PG 76-22) | -- | -- | 170 | FAIL | Optimum asphalt content was selected at 7.0%. Volumetric check at 7.0% AC resulted in a density of 96.5% meeting the minimum criteria of 96.5%. |
|  |  |  | 6.8% (PG 76-22) | -- | 3.3 @ 20000 | 1541 | PASS |  |
|  |  |  | 7.4% (PG 76-22) | -- | 10.3 @ 20000 | 3000 | PASS |  |
|  |  |  | 8.0% (PG76-22) | -- | 16.2 @ 20000 | -- | FAIL |  |
|  | Mix 2 CAM | 30% Grade 5 + 70% Man. Sand | 7.5% (PG76-22) | 94.6%(SGC) | 11.4 @ 20000 | 420 | FAIL | 8.1% was selected as the optimum asphalt content |
|  |  |  | 8.0% (PG76-22) | 96.2%(SGC) | 10.6 @ 20000 | 667 | FAIL |  |
|  | Mix 3 CAM | 45% Grade 5 + 30% Man. Sand + 25% Chat | 7.0% (PG76-22) | 97.1%(SGC) | 12.5 @ 18600 | 642 | FAIL | No optimum asphalt content could be obtained. |
|  |  |  | 7.5% (PG76-22) | 98.6%(SGC) | 12.5 @ 14000 | >1000 | FAIL |  |
|  | Mix 4 PFC | 100% Grade 5 + 0.3% Fibers | 6.0% (PG76-22) | 76.3% | 9.12 @ 10000 | >337 | PASS | 6.5% was the optimum asphalt content. |
|  |  |  | 6.5% (PG76-22) | 77.8% | 6.29 @ 10000 | >300 | PASS |  |
|  |  |  | 7.0% (PG76-22) | 78.4% | 8.50 @ 10000 | >1000 | PASS |  |
|  | Mix 5 PFC | 100% Grade 6 + 0.3% Fibers | 6.0% (PG76-22) | 75.7% | 11.09 @ 10000 | 246 | FAIL | 6.5% was the optimum asphalt content. |
|  |  |  | 6.5% (PG76-22) | 76.6% | 10.52 @ 10000 | 667 | PASS |  |
|  |  |  | 7.0% (PG76-22) | 77.2% | 12.56 @ 10000 | >720 | FAIL |  |
|  | Mix 6 SMA | 60% Grade 5 + 40% Man. Sand + 0.3% Fibers | 6.0% (PG76-22) | 96.8%(TGC) | 3.4 mm @ 20000 | 78 | FAIL | 7.2%AC was selected as the optimum asphalt content. |
|  |  |  | 6.5% (PG76-22) | 97.3%(TGC) | 3.9 mm @ 20000 | 157 | FAIL |  |
|  |  |  | 7.0% (PG76-22) | -- | 5.0 mm @ 20000 | 260 | FAIL |  |
|  |  |  | 7.2% (PG76-22) | 93.0%(SGC) | 6.6 mm @ 20000 | -- | -- |  |

Table A.  (Continued)

| Materials | Mix ID/Type | Combined Gradation | AC Content | Density | Hamburg Test | OT | Outcome | Remarks |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Hoban | Mix 7 CAM | 30% Grade 6 + 70% Man Sand | 9.0% (PG76-22) | -- | 3.08 mm @ 20000 | 189 | FAIL | Samples came from the District Lab. |
|  | Mix 8 CAM | 60% Hoban Grade 6 + 40% Rankin Screenings | 7.0% (PG 76-22) | -- | 2.1 mm @ 20000 | 83 | FAIL | 8.2% asphalt content was OK for HAM and OT,but not for volumetric. If volumetric was required, then 8.8% asphalt content would be the optimum. |
|  |  |  | 7.5% (PG 76-22) | 93.1%(SGC) | 2.1 mm @ 20000 | 243 | FAIL |  |
|  |  |  | 8.0% (PG 76-22) | 93.7%(SGC) | 2.3 mm @ 20000 | -- | -- |  |
|  |  |  | 8.5% (PG 76-22) | 95.5%(SGC) | 3.2 mm @ 20000 | 1068 | PASS |  |
|  | Mix 9 CAM | 65% Hoban Grade 6 + 35% Turner Screenings | 7.5% (PG 76-22) | 94.0%(SGC) | 2.5mm@20000 | 513 | FAIL | 7.8% asphalt content was OK for HAM and OT,but not for volumetric. To meet density requirement, 8.8% asphalt content is optimum. |
|  |  |  | 8.0% (PG 76-22) | 93.5%(SGC) | 3.0mm@20000 | 933 | PASS |  |
|  |  |  | 8.5% (PG 76-22) | 95.4%(SGC) | 5.0mm@20000 |  |  |  |
|  | Mix 10 PFC | 100% Grade 6 + 0.3% Fibers | 6.0% (PG76-22) | -- | 12.5 mm @ 4900 | 402 | FAIL | All the samples came from the District Lab, and the Air Void were around 26.5% |
|  |  |  | 6.5% (PG76-22) | -- | 8.1 mm @ 10000 | >450 | PASS |  |
|  |  |  | 7.0% (PG76-22) | -- | 12.5 @ 7000 | >1000 | NO PASS |  |
|  | Mix 11 SMA | 60% Hoban Grade 5 + 40% Turner Screenings + 0.3% Fbers | 6.0% (PG76-22) | 96.8%(TGC) | -- | -- | -- | 7.0%AC was selected as the optimum. |
|  |  |  | 6.5% (PG76-22) | 98.3%(TGC) | 2.3 mm @ 20000 | 28 | NO PASS |  |
|  |  |  | 7.0% (PG76-22) | 98.8%(TGC) | 2.6 mm @ 20000 | 300 | PASS |  |
|  |  |  |  | 96.7%(SGC) | 2.8 mm @ 20000 | -- | -- |  |
| Milligan | Mix 12 CAM | 50% F rock +49% Scrn +1% Lime | 6.5 (PG 70-22) | 95.0% (SGC) | 2.5 mm @ 20000 | 100 | FAIL | 7.2% AC was optimum |
|  |  |  | 7.5 (PG 70-22) | 97.1% @ 7.2% | 5.3 mm @ 20000 | 919 | PASS |  |
|  |  |  | 8.0 (PG 70-22) | -- | 14.3 mm @ 20000 | -- | -- |  |

Table A.  (Continued)

| Materials | Mix ID/Type | Combined Gradation | AC Content | Density | Hamburg Test |  | OT | Outcome | Remarks |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Zack Burk | Mix 13 CAM | 30% F rock + 69% Scrn + 1% lime | 6.0 (PG 70-22) | -- | 12.5 mm @ 14800 |  | 88 | FAIL | No optimum AC content could be obtained |
|  |  |  | 6.5 (PG 70-22) | -- | 12.5 mm@ 10000 |  | -- | FAIL |  |
|  |  |  | 7.0 (PG 70-22) | -- | 12.5 mm @ 9600 |  | -- | FAIL |  |
|  |  |  | 7.5 (PG 70-22) | -- | 12.5 mm @ 5900 |  | -- | FAIL |  |
| Duinick | Mix 14 CAM | 50% F rock + 24% DBI Man Sand +25% Thrasher Scrn + 1% Lime | 6.0 (PG 70-28) | -- | 12.5 mm @ 9000 |  | 743 | FAIL | No optimum AC content could be obtained |
|  |  |  | 6.5 (PG 70-28) | -- | 12.5 mm @ 6200 |  | -- | FAIL |  |
|  | Mix 15 CAM | 52% F rock + 47% Kiewit #7-#16 +1% lime | 6.0 (PG 70-28) | -- | 1.5 mm @ 15000 |  | 52 | FAIL | Based on Hamburg and Overlay Testing, an optimum of 7.2% AC was selected. However the density check at 7.2% asphalt was only 93.7%. |
|  |  |  | 6.5 (PG 70-28) | -- | 2.7 mm @ 15000 |  | -- |  |  |
|  |  |  | 7.0 (PG 70-28) | -- | 6.1 mm @ 15000 |  | 588 |  |  |
|  |  |  | 7.5 (PG 70-28) | -- | 16.1 mm @ 15000 |  | 1883 |  |  |
| Turner | Mix 16 CAM | 15% D rock + 20% F rock + 64% Scrng + 1% lime | 6.5 (PG 76-22) | -- | -- |  | 2 | FAIL | No optimum AC content could be obtained |
|  |  |  | 7.0 (PG 76-22) | -- | 3.89 mm @ 20000 |  | 19 | FAIL |  |
|  |  |  | 7.5 (PG 76-22) | -- | 5.36 mm @ 20000 |  | 72 | FAIL |  |
|  |  |  | 8.0 (PG 76-22) | -- | 5.46 mm @ 20000 |  | -- | -- |  |
| El Paso | CAM | District supplied Padre Canyon 3/8-inch and Scrngs. + Vado 3/8-inch | -- |  |  |  |  |  | No combination of these aggregates could meet gradation requirements for a CAM |
| * Designs shaded in blue were selected for placement at the Pecos Test Track. |  |  |  |  |  |  |  |  |  |

# SUMMARY REPORT OF LAB TESTING FOR PECOS PROJECT

# For each aggregate supplied to this project a balanced mix design was run to determine if there is an optimal asphalt content at which the competing requirement of meeting both the Hamburg and Overlay tester requirements are met.  The results obtained are summarized below

# 1. Eastland Rocks (Abilene)

## 1.1 The Aggregates and Binders

The Abilene district sent two shipments of aggregate from Vulcan’s Eastland quarry.  The first shipment was received in February, 2009 and included a Grade 6, manufactured sand and screenings as shown in Figure 1-1. A washed sieve analysis was performed on each aggregate as shown in Table 1-1. A PG76-22 asphalt binder from Alon was also provided.

(a) Grade 6                        (b) Manufactured Sand         (c) Screenings

Figure 1-1.  The First Shipment of Eastland Aggregates.

Table 1-1.  Eastland (First Shipment) Aggregate Gradations for Each Fraction (Cumulative Passing, %).

| Sieve Size | Grade 6 | Man. Sand | Screenings |
| --- | --- | --- | --- |
| 3/8 " | 100 | 100 | 99.5 |
| No. 4 | 54.6 | 99.9 | 82.5 |
| No. 8 | 2.6 | 73.7 | 57.7 |
| No. 16 | 1.4 | 39.6 | 40.4 |
| No. 30 | 1.3 | 21.1 | 29.3 |
| No. 50 | 1.3 | 10.7 | 22.9 |
| No. 200 | 1.2 | 3.2 | 15.8 |

The second set of samples was obtained in September, 2010 and there were four Eastland aggregate fractions: Grade 5, Grade 6, manufactured sand and chat as shown in the pictures in Figure 1-2. Washed sieve analyses are shown in Table 1-2. Asphalt binder received was a PG76-22S.

(a) Grade 5                   (b) Grade 6                      (c) Manufactured Sand   		(d) Chat

Figure 1-2.  The Second Shipment of Eastland Aggregates.

Table 1-2. Eastland (Second Shipment) Aggregate Gradations for Each Fraction (Cumulative Passing, %).

| Sieve Size | Grade 5 | Grade 6 | Man. Sand | Chat |
| --- | --- | --- | --- | --- |
| 3/8 " | 97.8 | 100.0 | 100.0 | 99.8 |
| No. 4 | 46.4 | 63.9 | 100.0 | 83.0 |
| No. 8 | 3.4 | 5.9 | 84.2 | 58.2 |
| No. 16 | 1.9 | 3.2 | 47.5 | 41.4 |
| No. 30 | 1.6 | 2.4 | 26.7 | 31.5 |
| No. 50 | 1.5 | 2.1 | 14.3 | 25.5 |
| No. 200 | 1.3 | 1.8 | 3.9 | 18.9 |

## 1.2 Eastland Mix Designs

### 1.2.1 MIX 1 - CAM Mix (1% Lime, Grade 6 + Man. sand + Screenings)

The Combined Gradation

This CAM mix comprised of 38% Grade 5, 33% Manufacture Sand, 28% Screenings and 1.0% Lime. The combined aggregate gradation was shown in Figure 1-3.

Figure 1-3. Associated Gradation for Eastland CAM Design (with Lime).

Performance Test and Optimum Asphalt Content

The Hamburg and Overlay Tests were conducted at four different asphalt contents: 6.2%, 6.8%, 7.4% and 8.0%.  Test results are listed in the Table 1-3. Photos of the specimens after Hamburg testing are shown in Figure 1-4.

Table 1-3. Summary of the Hamburg and Overlay Test Results.

| Asphalt Content | RICE | Hamburg Test |  |  | Overlay Test |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Air Void | Rutting Depth (mm) | Pass/Fail | Air Void | No. of cycles1 | Pass/Fail |
| 6.4% | 2.410 | -- | -- | -- | 6.4 / 6.8 | 170 | Fail |
| 6.8% | 2.398 | 7.5 / 7.3 | 3.3 @ 20000 | Pass | 6.4 / 6.3 | 1541 | Pass |
| 7.4% | 2.370 | 7.4 / 6.9 | 10.3 @ 20000 | Pass | 6.3 / 6.3 | 3000 | Pass |
| 8.0% | 2.355 | 7.6 / 7.4 | 16.1 @ 20000 | Fail | -- | -- | -- |
| 1: average of two or three samples testing |  |  |  |  |  |  |

Figure 1-4. Hamburg Test for Abilene Eastland CAM (with Lime).

From Figure 1-5, the acceptable asphalt content meeting both Hamburg-rutting and Overlay-cracking requirement ranges from 6.5 to 7.6 percent. Beyond 7.6 percent asphalt binder, the mixture will have rutting problems.  So, the initial selected OAC was 7.0%.

Optimum Asphalt Content

Figure 1-5. The Window of Acceptable Asphalt Content for Eastland CAM.

Volumetric Check

Two samples at 7.0% asphalt content were molded for the volumetric check. The test results are listed in Table 1-4 and the density from the theoretical maximum specific gravity was 96.5% and 96.6%, which meets the criteria of minimum density of 96.5%.

Table 1-4. Volumetric Check (SGC) at Initial Optimum Asphalt Content.

| Sample's No. | Theo. Max. Specific Gravity (Gt) | Sample Height (mm) | Weight of Dry Sample | Sample Weight in Water | Weight of Dry Surface | Density from Gt | Pass / Fail |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 7.0% AC_1 | 2.386 | 115 | 4587.3 | 2604.1 | 4596.6 | 96.5% | Pass |
| 7.0% AC_2 |  | 115 | 4591.6 | 2606.3 | 4599.1 | 96.6% | Pass |

Conclusion

A successful CAM mix design was developed using Vulcan Eastland aggregates in the following proportions:

- 38% Grade 6

- 33% Manufactured sand

- 28% Screenings

- 1%  Lime

- 7.0 percent PG 76-22

### 1.2.2 MIX 2 - CAM Mix (No Lime, Grade 5 + Man. sand)

The Combined Gradation

A second CAM mix design was attempted without lime (No Chat) using the second group materials received from the Eastland quarry. This CAM mix comprised of 30% Grade 5 and 70% manufacture sand. The combined aggregate gradation is shown in Figure 1-6.

Figure 1-6. Associated Gradation for Eastland CAM Design (No Lime, no Chat).

Performance Test

The Hamburg and Overlay Tests were conducted at two different asphalt contents: 7.5% and 8.0%.  Test results are listed in Table 1-5. Photos of specimens after Hamburg test are shown in Figure 1-7.

Table 1-5. Summary of Hamburg and Overlay Test Results.

| Asphalt Content | RICE | Density (SGC,%) | Hamburg Test |  |  | Overlay Test |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Air Void | Rutting Depth (mm) | Pass /Fail | Air Void | No. of cycles1 | Pass /Fail |
| 7.5% | 2.4068 | 94.6 | 7.3 / 7.3 | 11.4 @ 20000 | Pass | 8.2 / 7.8 | 420 | Pass |
| 8.0% | 2.3995 | 96.2 | 7.0 / 7.0 | 10.6 @ 20000 | Pass | 7.9 / 7.9 | 667 | Pass |
| 1: average of three samples testing |  |  |  |  |  |  |  |  |

Figure 1-7. Hamburg Test Specimens for Eastland CAM (No Lime, No Chat).

Conclusion

A second successful CAM mix design (without lime) was developed using Vulcan Eastland aggregates in the following proportions:

- 30% Grade 5

- 70% Manufactured sand

- 8.1 percent PG 76-22

### 1.2.3 MIX 3 - CAM Mix (No Lime, Grade 5 + Man Sand + Chat)

The Combined Gradation

A third CAM mix design was attempted including the Chat aggregate fraction without lime. This CAM mix was comprised of 45% Grade 5, 30% manufactured sand and 25% Chat. The combined aggregate gradation is shown in Figure 1-8.

Figure 1-8. Associated Gradation for Eastland CAM (No Lime, 25% Chat).

Performance Test

The Hamburg and Overlay tests were conducted  at two different asphalt contents: 7.5% and 8.0%.  Test results are listed in Table 1-6.

Table 1-6. Summary of Hamburg and Overlay Test Results.

| Asphalt Content | RICE | Density (SGC,%) | Hamburg Test |  |  | Overlay Test |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Air Void | Rutting Depth (mm) | Pass /Fail | Air Void | No. of cycles1 | Pass /Fail |
| 7.5% | 2.3913 | 97.1 | 6.3 / 6.5 | 12.5 @ 18600 | Fail | 6.4 / 6.2 | 642 | Fail |
| 8.0% | 2.3751 | 98.6 | 6.5 / 6.2 | 12.5 @ 14000 | Fail | 6.2 / 5.9 | >1000 | Pass |
| 1: average of three samples testing |  |  |  |  |  |  |  |  |

Conclusion

Based on Hamburg test results, no optimum asphalt content could be obtained with this combination of materials.

### 1.2.4 MIX 4 - Fine PFC Mix (No Lime, Grade 5 + Fibers)

The Combined Gradation

The Eastland Aggregates were used to design a fine-graded PFC mix was comprised of 100% Grade 5 and 0.3% fibers.

Performance Test

The Hamburg and Overlay tests were conducted at three different asphalt contents: 6.0%, 6.5% and 7.0%.  Test results are listed in Table 1-7. Photos of Hamburg specimens after testing are shown in Figure 1-9.

Table 1-7. Summary of  Hamburg and Overlay Test Results.

| Asphalt Content | RICE | Density (SGC, %) | Hamburg Test |  |  | Overlay Test |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Air Void | Rutting Depth (mm) | Pass /Fail | Air Void | No. of cycles1 | Pass /Fail |
| 6.0% | 2.4490 | 76.3 | -- | 9.12 @ 10000 | Pass | -- | 337 | Pass |
| 6.5% | 2.4311 | 77.8 | -- | 6.29 @ 10000 | Pass | -- | >350 | Pass |
| 7.0% | 2.4136 | 78.4 | -- | 8.50 @ 10000 | Pass | -- | >1000 | Pass |
| 1: average of two samples testing |  |  |  |  |  |  |  |  |

Figure 1-9. Hamburg Test for Eastland PFC (without Lime).

Lab Falling Head Permeability Test

The Falling Head Permeability test results are listed in the Table 1.

Table 1-8. The Falling Head Permeability Test Results.

| Times | 6.0% AC | 6.5% AC | 7.0% AC |  |
| --- | --- | --- | --- | --- |
| 1 | 2.94 | 3.69 | 4.40 |  |
| 2 | 2.97 | 3.68 | 4.31 |  |
| 3 | 3.00 | 3.69 | 4.31 |  |
| 4 | 2.91 | 3.68 | 4.47 |  |
| 5 | 2.91 | 3.72 | 4.44 |  |
| Average, s | 2.95 | 3.69 | 4.39 |  |
| Coefficient of Permeability, m/day | 78.3 | 62.1 | 52.1 |  |

Conclusion

6.5% was recommended as the optimum asphalt content for this Eastland PFC.

### 1.2.5 MIX 5 - PFC Mix (No Lime, Grade 6 + Fibers)

The Combined Gradation

This PFC mix was comprised of 100% Grade 6 and 0.3% Fibers.

Performance Test

The Hamburg and Overlay tests were conducted at three different asphalt contents: 6.0%, 6.5% and 7.0%.  Test results are listed in Table 1-9.

Table 1-9. The Hamburg and Overlay Test Results.

| Asphalt Content | RICE | Density (SGC,%) | Hamburg Test |  |  | Overlay Test |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Air Void | Rutting Depth (mm) | Pass /Fail | Air Void | No. of cycles1 | Pass /Fail |
| 6.0% | 2.4363 | 75.7 | -- | 11.09 @ 10000 | Pass | -- | 246 | Fail |
| 6.5% | 2.4187 | 76.4 | -- | 10.52 @ 10000 | Pass | -- | 667 | Pass |
| 7.0% | 2.4014 | 77.2 | -- | 12.56 @ 10000 | Fail | -- | >667 | Pass |
| 1: average of two samples testing |  |  |  |  |  |  |  |  |

Lab Falling Head Permeability Test

The Falling Head Permeability test results are listed in Table 1-10.

Table 1-10. The Falling Head Permeability Test Results.

| Times | 6.0% AC | 6.5% AC | 7.0% AC |  |
| --- | --- | --- | --- | --- |
| 1 | 3.37 | 3.56 | 3.69 |  |
| 2 | 3.47 | 3.59 | 3.75 |  |
| 3 | 3.41 | 3.53 | 3.75 |  |
| 4 | 3.41 | 3.53 | 3.69 |  |
| 5 | 3.35 | 3.56 | 3.65 |  |
| Average, s | 3.40 | 3.55 | 3.71 |  |
| Coefficient of Permeability, m/day | 69.3 | 65.6 | 62.9 |  |

Conclusion

An optimum asphalt content of 6.5% was recommended for this PFC design.  .

### 1.2.6 MIX 6 - SMA Mix (No Lime, Grade 5 + Man. sand + Fibers)

The Combined Gradation

A fine SMA mix was designed comprised of 60% Grade 5 and 40% manufacture sand, with 0.3% fibers. The combined aggregate gradation is shown in Figure 1-10.

Figure 1-10. Associated Gradation for Eastland SMA Design (without Lime).

Performance Test

The Hamburg and Overlay tests at three different asphalt contents: 6.0%, 6.5% and 7.0%.  These results are listed in the Table 1-11. Photos of the Hamburg specimens are shown in Figure 1-11.

Table 1-11. The Hamburg and Overlay Test Results.

| Asphalt Content | RICE | Density (TGC, %) | Hamburg Test |  |  | Overlay Test |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Air Void | Rutting Depth (mm) | Pass /Fail | Air Void | No. of cycles1 | Pass /Fail |
| 6.0% | 2.4345 | 96.8 | 7.3 / 7.2 | 3.4 @ 20000 | Pass | 7.6 / 7.5 | 78 | Fail |
| 6.5% | 2.4036 | 97.3 | 7.3 / 7.2 | 3.9 @ 20000 | Pass | 7.9 / 7.9 | 157 | Fail |
| 7.0% | 2.3727 | -- | 7.5 / 7.2 | 5.0 @ 20000 | Pass | 7.4 / 7.2 | 260 | Fail |
| 1: average of two samples testing |  |  |  |  |  |  |  |  |

Figure 1-11. Hamburg Test for Eastland SMA (without Lime).

Conclusion

7.2% was recommended as the optimum asphalt content for this Eastland SMA.

# 2. Hoban, Turner and Rankin Rocks (Odessa)

## 2.1 The Aggregates and Binders

The Odessa district also sent two shipments of aggregate. The first samples were received in April, 2009: Hoban Grade 6 and Hoban manufactured sand as shown in Figure 2-1.  Washed sieve analysis results are shown in Table 2-1. The asphalt binder was PG76-22 from Alon.

(a) Grade 6                                          (b) Manufactured sand

Figure 2-1. The First Group Hoban Aggregates.

Table 2-1. Aggregate Gradation for Fraction (Cumulative Passing, %).

| Sieve Size | Grade 6 | Manufacture sand |
| --- | --- | --- |
| 3/8 " | 100.0 | 99.9 |
| No. 4 | 61.3 | 99.6 |
| No. 8 | 11.1 | 87.9 |
| No. 16 | 1.7 | 68.7 |
| No. 30 | 0.7 | 48.3 |
| No. 50 | 0.6 | 26.2 |
| No. 200 | 0.5 | 6.8 |

The second group of samples arrived in September, 2010: Hoban Grade 5 and Hoban Grade 6. See pictures in Figure 2-2. Washed sieve analysis results are shown in Table 2-2. Asphalt binder was PG76-22S.

At this same time, three aggregates from the Rankin Pit were also sent (Grade 5, Grade 6 and Screenings) and two aggregates from the Turner Pit (Grade 5 and Screenings). See Figure 2-3 and Figure 2-4, Table 2-3 and Table 2-4 for more information on these aggregates.

(a) Grade 5                                       (b) Grade 6

Figure 2-2. The Second Group Hoban Aggregates.

(a) Grade 5                                (b) Grade 6                              (c) Screenings

Figure 2-3. The Rankin Pit Aggregates.

(a) Grade 5                               (b) Screenings

Figure 2-4. The Turner Pit Aggregates.

Table 2-2. The Gradation for Hoban Rock (Cumulative Passing, %).

| Sieve Size | Grade 5 | Grade 6 |
| --- | --- | --- |
| 3/8 " | 99.5 | 100.0 |
| No. 4 | 24.3 | 71.7 |
| No. 8 | 1.6 | 17.6 |
| No. 16 | 0.7 | 4.3 |
| No. 30 | 0.7 | 1.9 |
| No. 50 | 0.6 | 1.3 |
| No. 200 | 0.5 | 0.9 |

Table 2-3. The Gradation for Rankin Pit Rock (Cumulative Passing, %).

| Sieve Size | Grade 5 | Grade 6 | Screenings |
| --- | --- | --- | --- |
| 3/8 " | 99.1 | 100.0 | 100.0 |
| No. 4 | 36.0 | 48.5 | 99.6 |
| No. 8 | 3.7 | 3.2 | 81.6 |
| No. 16 | 3.1 | 2.6 | 58.2 |
| No. 30 | 2.9 | 2.5 | 43.2 |
| No. 50 | 2.7 | 2.5 | 33.0 |
| No. 200 | 2.5 | 2.4 | 21.2 |

Table 2-4. The Gradation for Turner Rock (Cumulative Passing, %).

| Sieve Size | Grade 5 | Screenings |
| --- | --- | --- |
| 3/8 " | 100.0 | 99.8 |
| No. 4 | 49.9 | 97.6 |
| No. 8 | 3.2 | 82.8 |
| No. 16 | 1.9 | 60.5 |
| No. 30 | 1.8 | 45.7 |
| No. 50 | 1.7 | 35.0 |
| No. 200 | 1.5 | 21.7 |

## 2.2 Mix Design

### 2.2.1 MIX 7 - CAM Mix (No Lime, Hoban Grade 6 + Hoban Man. sand)

The Combined Gradation

This CAM design was comprised of 50% Grade and 50% Manufactured sand. The combined aggregate gradation was shown in Figure 2-5.

Figure 2-5. Associated Gradation for Hoban CAM Design (No Lime).

Performance Test and Optimum Asphalt Content

The Hamburg and Overlay tests were conducted at four different asphalt contents: 6.8%, 7.4%, 8.0% and 8.6%.  These results are listed in the Table 2-5. Photos of the Hamburg specimens are shown in Figure 2-6.

Table 2-5. Summary of the Hamburg and Overlay Test Results.

| Asphalt Content | RICE | Hamburg Test |  |  | Overlay Test |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Air Void | Rutting Depth (mm) | Pass/Fail | Air Void | No. of cycles1 | Pass/Fail |  |
| 6.8% | 2.2813 | 8.1 / 7.9 | 2.47 mm @ 20000 | Pass | 7.9 / 7.5 | 152 | Fail |  |
| 7.4% | 2.2646 | 7.7 / 7.9 | 2.48 mm @ 20000 | Pass | 8.0 / 7.5 | 224 | Fail |  |
| 8.0% | 2.2432 | 8.0 / 8.0 | 2.72 mm @ 20000 | Pass | 7.0 / 7.4 | 571 | Fail |  |
| 8.6% | 2.2235 | 7.2 / 7.6 | 9.81 mm @ 20000 | Pass | 8.0 / 7.7 | 1857 | Pass |  |
| 1: average of two or three samples testing |  |  |  |  |  |  |  |

Figure 2-6. Hamburg Test for Hoban CAM (without Lime).

From Figure 2-7, the acceptable asphalt content meeting both Hamburg-rutting and Overlay-cracking requirement ranges from 8.14 to 8.64 percent. Beyond 8.64 percent asphalt binder, the mixture could have rutting problems. Therefore, the initial selected OAC was 8.4%.

Figure 2-7. The Window of Acceptable Asphalt Content for Hoban CAM.

Volumetric Check

Two samples at 8.2% and 8.4% asphalt content respectively were molded for the volumetric check. The test results are listed in Table 2-6 and the density from the theoretical maximum specific gravity was 95.7% and 95.8%, which did not meet the criteria of minimum 96.5%.

Table 2-6. Volumetric Check (SGC) at Initial Optimum Asphalt Content.

| Sample's No. | Theo. Max. Specific Gravity (Gt) | Sample Height (mm) | Weight of Dry Sample | Sample Weight in Water | Weight of Dry Surface | Density from Gt | Pass / Fail |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 8.2% AC_1 | 2.2341 | 114.9 mm | 4310.2 | 2301.3 | 4316.2 | 95.8% | Fail |
| 8.2% AC_2 |  | 114.8 mm | 4307.2 | 2299.2 | 4313.3 | 95.7% | Fail |
| 8.4% AC_1 | 2.2318 | 151.2 mm | 4317.0 | 2299.9 | 4320.6 | 95.7% | Fail |
| 8.4% AC_2 |  | 151.3 mm | 4309.1 | 2299.1 | 4314.0 | 95.8% | Fail |

Conclusion

No optimum asphalt content for this Hoban CAM. Alternative CAM designs were attempted as described below

### 2.2.2 MIX 8 - CAM Mix (No Lime, Hoban Grade 6 + Rankin Screenings)

The Combined Gradation

This CAM mix was comprised of 60% Hoban Grade 6 and 40% Rankin Pit Screenings. The combined aggregate gradation is shown in Figure 2-8.

Figure 2-8. Associated Gradation for Hoban and Rankin CAM Design.

Performance Test

The Hamburg and Overlay tests were conducted at four different asphalt contents:7.0%, 7.5%, 8.0% and 8.5%.  Results are listed in Table 2-7. Photos of the Hamburg specimens are shown in Figure 2-9.

Table 2-7. The Hamburg and Overlay Test Results.

| Asphalt Content | RICE | Density (SGC) | Hamburg Test |  |  | Overlay Test |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Air Void | Rutting Depth (mm) | Pass /Fail | Air Void | No. of cycles1 | Pass /Fail |
| 7.0% | 2.3311 | 91.1% | 6.4 / 6.4 | 2.1 mm @ 20000 | Pass | 6.5 / 6.7 | 83 | Fail |
| 7.5% | 2.3143 | 92.2% | 6.4 / 6.3 | 2.1 mm @ 20000 | Pass | 6.4 / 6.4 | 243 | Fail |
| 8.0% | 2.2913 | 93.5% | 6.1 / 6.3 | 2.3 mm @ 20000 | Pass | -- | -- | -- |
| 8.5% | 2.2767 | 95.4% | 6.4 / 6.3 | 3.2 mm @ 20000 | Pass | 6.3 / 6.5 | 1068 | Pass |
| 1: average of two samples testing |  |  |  |  |  |  |  |  |

Figure 2-9. Hamburg Test for Hoban and Rankin CAM.

Conclusion

Since the volumetric at 8.5% asphalt content was only 95.4%, so 8.8% asphalt content was recommended as the optimum asphalt content based on extensional interpolating for this CAM.

### 2.2.3 MIX 9 - CAM Mix (No Lime, Hoban Grade 6 + Turner Screenings)

The Combined Gradation

This CAM mix comprised of 65% Hoban Grade 6 and 35% Turner Pit Screenings. The combined aggregate gradation is shown in Figure 2-10.

Figure 2-10. Associated Gradation for Hoban and Turner CAM Design.

Performance Test

The Hamburg and Overlay tests were conducted at four different asphalt contents:, 7.0%, 7.5%, 8.0% and 8.5% .  Results are shown in Table 2-8 and Figure 2-11.

Table 2-8. The Hamburg and Overlay Test Results.

| Asphalt Content | RICE | Density (SGC) | Hamburg Test |  |  | Overlay Test |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Air Void | Rutting Depth (mm) | Pass /Fail | Air Void | No. of cycles1 | Pass /Fail |
| 7.5% | 2.3016 | 93.7% | 6.1 / 6.3 | 2.5mm@20000 | Pass | 6.5 / 6.6 | 513 | Fail |
| 8.0% | 2.2972 | 93.8% | 6.3 / 6.3 | 3.0mm@20000 | Pass | 6.5 / 6.9 | 933 | Pass |
| 8.5% | 2.2803 | 95.5% | 6.5 / 6.9 | 5.0mm@20001 | Pass | -- | -- | -- |
| 1: average of two samples testing |  |  |  |  |  |  |  |  |

Figure 2-11. Hamburg Test for Hoban and Turner Pit CAM.

Conclusion

Since the volumetric at 8.5% asphalt content was only 95.5%, so 8.8% asphalt content was recommended as the optimum asphalt content based on extrapolation for this CAM.

### 2.2.4 MIX 10 - PFC Mix (No Lime, Hoban Grade 6 + Fibers)

The Combined Gradation

A fine-graded PFC mix was designed without lime using the second shipment of Hoban materials. This PFC mix was comprised of 100% Grade 6 and 0.3% fibers.

Performance Test

The Hamburg and Overlay tests were conducted at three different asphalt contents: 6.0%, 6.5% and 7.0%.  Results are shown in Table 2-9. These samples were prepared by the Odessa district lab and shipped to TTI.

Table 2-9. The Hamburg and Overlay Test Results.

| Asphalt Content | RICE | Density (SGC, %) | Hamburg Test |  |  | Overlay Test |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Air Void | Rutting Depth (mm) | Pass /Fail | Air Void | No. of cycles1 | Pass /Fail |
| 6.0% | -- | -- | 26.4 / 26.7 | 12.5 @ 4900 | Fail | -- | 402 | Pass |
| 6.5% | -- | -- | 26.2 / 26.9 | 8.1 @ 10000 | Pass | -- | >450 | Pass |
| 7.0% | -- | -- | 26.5 / 26.6 | 12.5 @ 7000 | Fail | -- | >1000 | Pass |
| 1: average of two samples testing |  |  |  |  |  |  |  |  |

Conclusion

6.5% was recommended as the optimum asphalt content for this Hoban PFC.

### 2.2.5 MIX 11 - SMA Mix (No Lime, Hoban Grade 5 + Turner Scr. + Fibers)

The Combined Gradation

This SMA mix comprised of 60% Hoban Grade 5 and 40% Turner Screenings, with 0.3% Fibers. The combined aggregate gradation was shown in Figure 2-12.

Figure 2-12. Associated Gradation for Hoban and Turner SMA Design.

Performance Test

The Hamburg and Overlay tests were conducted at three different asphalt contents: 6.0, 6.5% and 7.0%.  Results are shown in Table 2-10 and Figure 2-13. .

Table 2-10. the Hamburg and Overlay Test Results.

| Asphalt Content | RICE | Density (TGC, %) | Hamburg Test |  |  | Overlay Test |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Air Void | Rutting Depth (mm) | Pass /Fail | Air Void | No. of cycles1 | Pass /Fail |
| 6.0% | 2.341 | 96.8 | -- | -- | -- | -- | -- | -- |
| 6.5% | 2.327 | 98.3 | 6.0 / 6.0 | 2.3mm @ 20000 | Pass | 5.9 / 5.9 | 28 | Fail |
| 7.0% | 2.308 | 98.8 | 5.8 / 5.8 | 2.6mm @ 20000 | Pass | 5.6 / 5.7 | 300 | Pass |
| 1: average of two samples testing |  |  |  |  |  |  |  |  |

Figure 2-13. Hamburg Test for Hoban and Turner SMA (No Lime).

Conclusion

7.0% was recommended as the optimum asphalt content for this SAM.

# 3. Milligan Rocks (Amarillo District)

## 3.1 The Aggregates and Binders

The Amarillo district sent aggregates from the Milligan Pit: an F Rock and Screening.  Photos are shown in Figure 3-1. Washed sieve analysis results are shown in Table 3-1. Asphalt binder was a PG70-22 from Alon.

(a) F Rock                                            (b) Screenings

Figure 3-1. The Milligan Aggregates.

Table 3-1. Aggregate Gradation for Each Fraction (Cumulative Passing, %).

| Sieve Size | F Rock | Screenings |
| --- | --- | --- |
| 3/8 " | 100.0 | 99.9 |
| No. 4 | 61.6 | 99.9 |
| No. 8 | 4.5 | 85.1 |
| No. 16 | 1.8 | 59.6 |
| No. 30 | 1.4 | 42.0 |
| No. 50 | 1.2 | 28.2 |
| No. 200 | 0.8 | 9.4 |

## 3.2 MIX 12 - CAM Mix Design (1% Lime, F rock + Screenings)

The Combined Gradation

This CAM mix was comprised of 50% F Rock, 49% Screenings and 1.0% Lime. The combined aggregate gradation is shown in Figure 3-2.

Figure 3-2. Associated Gradation for Milligan CAM Design (with Lime).

Performance Test and Optimum Asphalt Content

The Hamburg and Overlay tests were conducted at three different asphalt contents: 6.5%, 7.5%, 8.0%.  Results are shown in Table 3-2 and Figure 3-3.

Table 3-2. Summary of the Hamburg and Overlay Test Results.

| Asphalt Content | RICE | Hamburg Test |  |  | Overlay Test |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Air Void | Rutting Depth (mm) | Pass/Fail | Air Void | No. of cycles1 | Pass/Fail |  |
| 6.5% | 2.3948 | 7.9 / 7.7 | 2.5 mm @ 20000 | Pass | 7.0 / 7.0 | 100 | Fail |  |
| 7.5% | 2.3639 | 7.7 / 7.9 | 5.3 mm @ 20000 | Pass | 7.2 / 7.5 | 919 | Pass |  |
| 8.0% | 2.3314 | 7.7 / 7.8 | 14.3 mm @ 20000 | Fail | -- | -- | -- |  |
| 1: average of two or three samples testing |  |  |  |  |  |  |  |

Figure 3-3. Hamburg Test for Milligan CAM.

From Figure 3-4, the acceptable asphalt content meeting both Hamburg-rutting and Overlay-cracking requirement ranges from 6.4 to 7.9 percent. Beyond 7.9 percent asphalt binder, the mixture could have rutting problems.  Therefore, the initial selected OAC was 7.2%.

Figure 3-4. The Window of Acceptable Asphalt Content for Milligan CAM.

Volumetric Check

Two samples at 6.5% and 7.2% asphalt content respectively were molded for the volumetric check. The test results were listed in Table 3-3 and the density from the theoretical maximum specific gravity was 95.0% and 97.0%.

Table 3-3. Volumetric Check (SGC) at Initial Optimum Asphalt Content.

| Sample's No. | Theo. Max. Specific Gravity (Gt) | Sample Height (mm) | Weight of Dry Sample | Sample Weight in Water | Weight of Dry Surface | Density from Gt | Pass / Fail |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 6.5% AC_1 | 2.395 | 116.5 | 4617.6 | 2599 | 4629.1 | 95.0% | Fail |
| 6.5% AC_2 |  | 116.4 | 4607.8 | 2592.3 | 4619.3 | 94.9% | Fail |
| 7.2% AC_1 | 2.366 | 114.1 | 4567.7 | 2584 | 4572.6 | 97.1% | Pass |
| 7.2% AC_2 |  | 114.2 | 4564.4 | 2579.8 | 4569.3 | 97.0% | Pass |

Conclusion

7.2% was the optimum asphalt content by the balance mix design method.

# 4. Zack Burkett (Wichita Falls)

## 4.1 The Aggregates and Binders

The Wichita Falls District sent three aggregates from the Zack Burkett quarry: F Rock, manufactured sand and screenings as shown in Figure 4-1. Results of washed sieve analyses are shown in Table 4-1. The asphalt binder was a PG70-22 from Valero.

(a) F Rock                                 (b) Manufacture Sand                  (c) Screenings

Figure 4-1. The Zack Burkett Aggregates.

Table 4-1. The Gradation for Each Rock (Cumulative Passing, %).

| Sieve Size | F Rock | Manufacture Sand | Screenings |
| --- | --- | --- | --- |
| 3/8 " | 100.0 | 100.0 | 100.0 |
| No. 4 | 51.5 | 99.6 | 98.7 |
| No. 8 | 3.8 | 79.1 | 59.6 |
| No. 16 | 2.6 | 39.9 | 29.1 |
| No. 30 | 2.6 | 16.3 | 17.3 |
| No. 50 | 2.5 | 5.5 | 12.3 |
| No. 200 | 2.4 | 2.9 | 8.1 |

## 4.2 MIX 13 - CAM Mix Design (1% Lime, F rock + Screenings)

The Combined Gradation

This CAM mix was comprised of 30% F Rock, 69% Screenings and 1.0% lime. The combined aggregate gradation is shown in Figure 4-2.

.

Figure 4-2. Associated Gradation for Wichita Falls CAM Design (with Lime).

Performance Test and Optimum Asphalt Content

The Hamburg tests were conducted at four different asphalt contents: 6.0%, 6.5%, 7.5%, 8.0% .  Results are listed in Table 3-2. Since all the rutting depths failed the criteria of 12.5@15000, only one sample at 6.0% asphalt content was run the overlay test. The Hamburg specimens are shown in Figure 4-3.

Table 4-2. Summary of the Hamburg and Overlay Test Results.

| Asphalt Content | RICE | Hamburg Test |  |  | Overlay Test |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Air Void | Rutting Depth (mm) | Pass/Fail | Air Void | No. of cycles1 | Pass/Fail |  |
| 6.0% | 2.3921 | 7.2 / 7.1 | 12.5 mm @ 14800 | Fail | 6.2 | 88 | Fail |  |
| 6.5% | 2.3780 | 7.0 / 7.0 | 12.5 mm @ 10000 | Fail | -- | -- | -- |  |
| 7.0% | 2.3618 | 7.3 / 7.2 | 12.5 mm @ 9600 | Fail | -- | -- | -- |  |
| 7.5% | 2.3449 | 7.3 / 6.9 | 12.5 mm @ 5900 | Fail | -- | -- | -- |  |
| 1: average of two or three samples testing |  |  |  |  |  |  |  |

Figure 4-3. Hamburg Test for Wichita Falls CAM.

Conclusion

No optimum asphalt content can be obtained.  It is recommended that alternative aggregates be used.  Also at the Districts request only a PG 70-22 binder was used.  Future designs should evaluate the use of a PG 76-22.

# 5. Duininck, Dbi, Thrasher and Kiewit Rocks (Lubbock)

## 5.1 The Aggregates and Binders

The Lubbock district submitted five aggregates:  Duininck F Rock, DBI manufactured sand, Thrasher Screenings,  Kiewit ¼”-#7 and Kiewit #7-#16.  Photos of the aggregates are shown in Figure 5-1. Washed sieve analysis results are shown in Table 5-1. The asphalt binder submitted was PG70-28 from Valero.

(a) F Rock                                   (b) Manufactured sand                  (c) Screenings

(d) ¼”_#7                                    (e) #7-#16

Figure 5-1. The Milligan Aggregates.

Table 5-1. Aggregate Gradation for Each Fraction (Cumulative Passing, %).

| Sieve Size | F Rock | Manufacture Sand | Screenings | ¼”_#7 | #7-#16 |
| --- | --- | --- | --- | --- | --- |
| 3/8 " | 100.0 | 99.8 | 99.8 | 100.0 | 100.0 |
| No. 4 | 60.8 | 97.7 | 98.9 | 85.0 | 99.9 |
| No. 8 | 2.0 | 72.4 | 86.8 | 12.6 | 85.2 |
| No. 16 | 0.7 | 48.6 | 69.6 | 3.8 | 54.8 |
| No. 30 | 0.5 | 32.8 | 56.5 | 3.1 | 39.3 |
| No. 50 | 0.5 | 17.4 | 41.6 | 2.7 | 30.4 |
| No. 200 | 0.4 | 3.3 | 18.9 | 1.9 | 12.2 |

## 5.2 MIX 14 - CAM Mix Design (1% Lime, F rock + Man Sand + Screenings)

The Combined Gradation

This CAM mix comprised of 50% Duininck F Rock, 24% DBI manufactured sand, 25% Thrasher screenings and 1.0% lime. The combined aggregate gradation is shown in Figure 5-2.

Figure 5-2. Associated Gradation for Lubbock CAM Design (with Lime).

Performance Test and Optimum Asphalt Content

The Hamburg and Overlay tests were conducted at two different asphalt contents: 6.0% and 6.5%.  Results are listed in the Table 5-2. Photos of Hamburg specimens are shown in Figure 5-3 (marked as Lubbock B).

Table 5-2 .Summary of the Hamburg and Overlay Test Results.

| Asphalt Content | RICE | Hamburg Test |  |  | Overlay Test |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Air Void | Rutting Depth (mm) | Pass/Fail | Air Void | No. of cycles1 | Pass/Fail |  |
| 6.0% | 2.4054 | 7.6 / 7.5 | 12.5 mm @ 9000 | Fail | 7.3 / 7.3 | 743 | Pass |  |
| 6.5% | 2.3900 | 7.2 / 7.4 | 12.5 mm @ 6200 | Fail | -- | -- | -- |  |
| 1: average of two or three samples testing |  |  |  |  |  |  |  |

Figure 5-3. Hamburg Test for Lubbock CAM.

Conclusion

No optimum asphalt content by balance design can be obtained.

## 5.3 MIX 15 - CAM Mix Design (1% Lime, F rock + #7-#16)

The Combined Gradation

This CAM mix comprised of 52% Duininck F Rock, 47% Kiewit #7-#16 and .0% Lime. The combined aggregate gradation was shown in Figure 5-4.

Figure 5-4. Associated Gradation for Lubbock CAM Design (with Lime).

Performance Test and Optimum Asphalt Content

The Hamburg and Overlay tests were conducted at four different asphalt contents: 6.0%, 6.5%, 7.0% and 7.5%.  Results are listed in the Table 5-3. Some of the Hamburg specimens are shown in Figure 5-3.

Table 5-3. Summary of the Hamburg and Overlay Test Results.

| Asphalt Content | RICE | Hamburg Test |  |  | Overlay Test |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Air Void | Rutting Depth (mm) | Pass/Fail | Air Void | No. of cycles1 | Pass/Fail |  |
| 6.0% | 2.3238 | 7.3 / 7.2 | 1.5 mm @ 15000 | Pass | 6.8 / 6.8 | 52 | Fail |  |
| 6.5% | 2.3091 | 7.1 / 7.3 | 2.7 mm @ 15000 | Pass | -- | -- | -- |  |
| 7.0% | 2.2900 | 7.3 / 7.0 | 6.1 mm @ 15000 | Pass | 6.7 / 6.8 | 588 | Fail |  |
| 7.5% | 2.2777 | 7.4 / 6.9 | 16.1 mm @ 15000 | Fail | 6.9 / 6.8 | 1883 | Pass |  |
| 1: average of two or three samples testing |  |  |  |  |  |  |  |

From Figure 5-5, acceptable asphalt content meeting both Hamburg-rutting and Overlay-cracking requirement ranges from 7.1 to 7.3 percent. Beyond 7.3 percent asphalt binder, the mixture could have rutting problems. Therefore, the initial selected OAC was 7.2%.

Figure 5-5. The Window of Acceptable Asphalt Content for Lubbock CAM.

Volumetric Check

Two samples at 7.2% asphalt content were molded for the volumetric check. The test results are listed in Table 5-4 and the density from the theoretical maximum specific gravity was determined to be 93.7%.

Table 5-4. Volumetric Check (SGC) at Initial Optimum Asphalt Content.

| Sample's No. | Theo. Max. Specific Gravity (Gt) | Sample Height (mm) | Weight of Dry Sample | Sample Weight in Water | Weight of Dry Surface | Density from Gt | Pass / Fail |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 7.2% AC_1 | 2.285 | 118.6 | 4410.4 | 2368.8 | 4425.8 | 93.8% | Fail |
| 7.2% AC_2 |  | 118.7 | 4409.9 | 2366.1 | 4427.7 | 93.6% | Fail |

Conclusion

No optimum asphalt content can be obtained.  It is suggested that the future designs be run with a PG 76-22 binder

# 6. Turner Pit Rock (San Angelo)

## 6.1 The Aggregates and Binders

The San Angelo District submitted five Turner Pit aggregate fractions:  F Rock, Screenings, Grade 3, D Rock and Blow Sand (Figure 6-1). Washed sieve analyses were performed on the F Rock, Screenings, and D Rock (Table 6-1). Asphalt binder was a PG76-22 from Alon.

(a) F Rock                                   (b) Screenings                        (c) Grade 3

(d) D Rock                                    (e) Blow Sand

Figure 6-1. The Turnepit Aggregates (San Angelo).

Table 6-1. Aggregate Gradation for Each Fraction (Cumulative Passing, %).

| Sieve Size | F Rock | D Rock | Screenings |
| --- | --- | --- | --- |
| 3/8 " | 100.0 | 92.8 | 100.0 |
| No. 4 | 82.9 | 10.3 | 99.5 |
| No. 8 | 3.0 | 1.3 | 84.4 |
| No. 16 | 2.2 | 1.2 | 61.8 |
| No. 30 | 2.0 | 1.2 | 47.1 |
| No. 50 | 2.0 | 1.2 | 36.4 |
| No. 200 | 1.8 | 1.1 | 22.8 |

## 6.2 MIX 16 - CAM Mix Design (1% Lime, D rock + F rock + Screenings)

The Combined Gradation

This CAM mix was comprised of 15% D Rock, 20% F Rock, 64% Screenings and 1.0% lime. The combined aggregate gradation is shown in Figure 6-2.

Figure 6-2. Associated Gradation for Turner pit CAM Design (with Lime).

Performance Test and Optimum Asphalt Content

The Hamburg and Overlay tests were conducted at four different asphalt contents: 6.5%, 7.0%, 7.5% and 8.0%. The results are listed in the Table 6-2. Since the OT cycles were too low even at 7.5% asphalt content, no further tests were performed.

Table 6-2. Summary of the Hamburg and Overlay Test Results.

| Asphalt Content | RICE | Hamburg Test |  |  | Overlay Test |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Air Void | Rutting Depth (mm) | Pass/Fail | Air Void | No. of cycles1 | Pass/Fail |  |
| 6.5% | 2.3812 | -- | -- | -- | 7.1 / 6.9 | 2 | No |  |
| 7.0% | 2.3456 | 7.0/6.9 | 3.89 @ 20000 | Pass | 7.0 / 6.8 | 19 | No |  |
| 7.5% | 2.3378 | 7.0/6.9 | 5.36 @ 20000 | Pass | 6.8 / 6.8 | 72 | No |  |
| 8.0% | 2.3158 | 7.0/7.0 | 5.46 @ 20001 | Pass | -- | -- | -- |  |
| 1: average of two or three samples testing |  |  |  |  |  |  |  |

Conclusion

No optimum asphalt content can be obtained.  Poor performance in the Overlay tester is an indication of a aggregate/binder compatibility problems, recommend changing aggregate types.

# 7. EL Paso Rock (No Mix Design)

## 7.1 The Aggregates and Binders

The El Paso District provided four aggregates: 3/8” Padre Canyon, Padre Canyon Screenings, 3/8” Vado and Vado Screenings.  (Figure 7-1).  Results of the washed sieve analyses are shown in Table 7-1. An asphalt Binder PG 70-22 from TK was also provided.  Unfortunately, no combination of the aggregates submitted would meet the gradation requirements for a CAM.  Need alternative aggregate for future CAM designs.

(a) 3/8” Padre Canyon                       (b) Padre Canyon Screenings

(c) 3/8” Vado                                       (d) Vado Screenings

Figure 7-1. The EL Paso Aggregates.

Table 7-1. The Gradation for Each Rock (Cumulative Passing, %).

| Sieve Size | 3/8” Rock Padre Canyon | Screenings Padre Canyon | 3/8” Rock Vado | Screenings Vado |
| --- | --- | --- | --- | --- |
| 3/8 " | 87.9 | 100.0 | 94.8 | 100.0 |
| No. 4 | 9.7 | 99.6 | 36.8 | 89.8 |
| No. 8 | 2.3 | 83.2 | 4.2 | 66.5 |
| No. 16 | 1.6 | 58.9 | 2.4 | 49.4 |
| No. 30 | 1.5 | 40.6 | 2.3 | 37.5 |
| No. 50 | 1.5 | 27.9 | 2.2 | 28.6 |
| No. 200 | 1.2 | 12.5 | 2.0 | 17.1 |