Transportation Infrastructure Precast Innovation Center

(TRANS-IPIC)

University Transportation Center (UTC)

Bio-Inspired Solutions for Jersey and Road Noise Barriers: Exploring 3D Printing as Alternative Precast Technology

PU-23-RP-03

Quarterly Progress Report

For the performance period ending [10/01/2024]

Submitted by:

Jan Olek1(olek@purdue.edu),

Jeff Youngblood2(jpyoungb@purdue.edu),

Pablo Zavattieri1(zavattie@purdue.edu )

1Lyles School of Civil Engineering, Purdue University

2School of Materials Engineering, Purdue University

Collaborators / Partners:

Terran Robotics

RCAM technology

Submitted to:

TRANS-IPIC UTC

University of Illinois Urbana-Champaign

Urbana, IL

TRANS-IPIC Quarterly Progress Report:

Project Description:

- Research Plan - Statement of Problem

The continuous improvement of transportation infrastructure is essential for ensuring the safety of road users and maintaining the efficiency of the transportation network. A critical element of this enhancement is the incorporation of impact-resistant structures in the construction and retrofitting of infrastructure components, such as roadside barriers. Recently, the growing prevalence of electric vehicles (EVs) presents significant challenges to the performance and safety of these barriers. Due to their increased weight, primarily from large batteries, electric vehicles (EVs) generate greater impact forces that conventional barriers are not designed to withstand [1]-[5]. Recent crash tests have shown that current barriers, which are optimized for lighter gasoline-powered vehicles, often fail to contain heavier EVs, leading to catastrophic consequences [1]-[5]. For instance, as shown in Fig. 1, a 7,000-pound Rivian R1T truck crushed and tore through concrete barriers commonly used as freeway median barriers or to shield highway construction workers from ongoing traffic, with minimal deceleration, posing significant risks to both passengers and infrastructure [1][2]. This issue is due to the fact that EVs can weigh 20% to 50% more than traditional vehicles, drastically increasing the energy transferred during collisions [1][2].

As EVs become a larger portion of the vehicle fleet, enhancing the energy absorption capacity and impact resistance of roadside barriers has become urgent and essential. Developing more robust barrier designs capable of handling these heavier loads is critical not only for public safety but also for preserving transportation infrastructures, which are not currently designed to accommodate vehicles of such weight. Cody Stolle, Assistant Director of the Midwest Roadside Safety Facility, mentioned that researchers at the facility are working on a new barrier system designed to accommodate a wider range of vehicles [3]. Additionally, Mick Syslo, Deputy Director at the Nebraska Department of Transportation, noted that "thousands of miles" of guardrails and barriers may need to be replaced to meet evolving safety requirements [4].

In our project, we aim to utilize 3D printing technology and bio-inspired design principles to enhance the energy absorption capacity of concrete barriers, thereby improving their ability to ensuring future roadway safety. We have demonstrated the ability to make concrete barriers both stronger and more energy-absorbing under impact conditions— a breakthrough achieved by combining clever architectures inspired by extreme animals in nature with 3D concrete printing technology.

Fig-1. A 7,000-pound Rivian R1T truck crushed and tore through concrete barriers commonly used as freeway median barriers or to shield highway construction workers from ongoing traffic, with minimal deceleration, posing significant risks to both passengers and infrastructure [1][2].

- Research Plan - Summary of Project Activities (Tasks)

Task 1: Fabrication

Task 1.1: Develop a specialized printing head for accurate deposition of concrete in a layer-by-layer fashion, optimizing for strength, durability, and high-strength structures for both LALS and LSRA printers.

Task 1.2: Design and fabricate a printing head for extruding polymeric material, strategically integrating it into the biomimetic Jersey barrier design to create energy-absorbing weak interfaces. During our first year, we will implement this in our LALS printer and will plan our implementation for the LSRA printer in subsequent years.

Task 2: Architected Material Designs

Task 2.1: Develop biomimetic architectures inspired by nature to optimize energy dissipation in the Jersey barriers, incorporating weak interfaces, cellular structures, and geometric patterns using both LALS and LSRA printers.

Task 2.2: Study and develop architected materials specifically tailored for acoustic barriers, aiming to mitigate road/traffic noise and the use of shape-shifting materials for reconfigurable barriers that can adapt to different noise patterns and frequency spectra variations.

Task 3: Material Characterization and Testing

Tasks 3.1: Conduct comprehensive material characterization and testing of the 3D printed biomimetic Jersey barriers, including mechanical tests to assess strength, deformation behavior, and energy absorption capacity under quasi-static conditions. Additionally, perform dynamic (drop-tower) impact tests to evaluate performance in simulated collision scenarios.

Tasks 3.2: Evaluate efficiency of reconfigurable traffic noise barriers based on shape-shifting materials using low-cost DIY impedance tube testing to measure sound absorption and transmission loss of the barriers in a controlled environment.

| Project Milestones (assuming August 1 Start Date and a 12 month project) |  | 2023-2024 |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 |
| 1 | Task 1.1 (100% completed) |  |  |  |  |  |  |  |  |  |  |  |  |
| 2 | Tasks 1.2(100% completed) |  |  |  |  |  |  |  |  |  |  |  |  |
| 3 | Task 2.1(100% completed) |  |  |  |  |  |  |  |  |  |  |  |  |
| 4 | Task 2.2(100% completed) |  |  |  |  |  |  |  |  |  |  |  |  |
| 5 | Task 3.1(100% completed) |  |  |  |  |  |  |  |  |  |  |  |  |
| 6 | Task 3.2(100% completed) |  |  |  |  |  |  |  |  |  |  |  |  |
| 4 | PI Submits Final DRAFT report to TRANS-IPIC for editing and publication(waiting for TRANS-IPIC to send the final report formant) |  |  |  |  |  |  |  |  |  |  |  |  |
| 5 | Report Posted to TRANS-IPIC website |  |  |  |  |  |  |  |  |  |  |  |  |

Project Progress:

- Progress for each research task

Task 1: Fabrication

Task 1.1: 100% completed- please reference to previous quarterly reports

Task 1.2: 100% completed

In this study, we aimed to explore the fabrication method for printing cement and polymer materials to create functional composite materials. We utilized syringe extrusion to integrate silicone with cement using a small-scale printer (Fig. 2a and 2b). The silicone exhibited suitable rheological properties for extrusion, though challenges with its buildability were noted. To address this, we designed a toolpath geometry that positions the silicone between cement filaments, allowing the cement to support the load of previous layers (Fig. 2(a) and (b)). The cement-silicone composite was designed to create hard-soft material interfaces to optimize energy absorption capacity. Mechanical performance was evaluated through three-point bending flexural tests. As shown in Fig. 2c, the 3D-printed cement samples exhibited brittle failure upon reaching peak load, while the composite samples, consisting of both cement and silicone, displayed multiple small load drops in the load-displacement curves. This behavior suggests the formation of multiple cracks rather than a single catastrophic failure. Fig. 2d presents the fracture pattern of the sample, which shows multiple cracks formation as well as strong scratch-recovery behavior due to the presence of silicone. The results demonstrate that by combining polymer with cement, a highly stretchable composite with enhanced energy absorption capacity can be created, outperforming cement-only samples.

This achievement is significant for the continuation of the project. However, further work is needed to improve the buildability of polymer materials. Future efforts should focus on enhancing the rheological properties of the polymer, possibly through polymer synthesis or increasing solid content. The ability to print both polymer and cement opens up opportunities to optimize energy absorption in materials for roadside barriers. In nature, hard-soft interfaces are used to dissipate energy effectively. For example, the integration of flexible polymeric nanofibers with rigid mineral components results in a periodic variation in stiffness [9]. When this feature is combined with the helicoidal (Bouligand) architecture, it promotes crack twisting, thereby increasing the material's ability to resist fracture and absorb more energy [9].  In phase one of this study, architected materials were designed using a single material (fiber-reinforced mortar). Now, with the capability to 3D print two materials, we could incorporate soft polymers into cement structures during the printing process, mimicking nature’s hard-soft material combinations. This could further optimize energy absorption properties. Furthermore, 3D printing with polymer-cement materials offers the potential to develop phase-transforming cellular materials with reconfigurable properties for the proposed reconfigurable noise barrier in this project. These materials could function as actuators, dynamically adjusting the periodic arrangement of phononic crystal structures to optimize noise mitigation based on varying conditions such as vehicle type, speed, and construction activities.

Fig-2. (a) Schematic illustrated 3D printing of cement and silicone using syringe extrusion. (b) Examples of cement-silicone composite samples fabricated by small scale 3D printer(c) Load-displacement curve from the three-point bending test for 3D-printed samples: cement-only and cement-silicone composite(d) fractured sample showing highly scratch behavior

Task 2: Architected Material Designs

Task 2.1: 100% completed- please reference to previous quarterly reports

Task 2.2: 100% completed

Noise is pervasive in various environments, originating from sources like rooms, industries, roads, airports, and other forms of transportation. Traffic noise frequencies fluctuate based on factors such as vehicle types, weather, road conditions, and traffic flow. Studies have shown that these variations in traffic conditions can cause the dominant noise frequencies to shift between 500 and 1200 Hz [6][7]. Traditional barriers, such as vertical walls, have several drawbacks. Firstly, they are heavy and can impose significant loads and moments on their foundations. Secondly, when oblique sound waves strike these barriers, they often cause increased diffraction at the top edge, allowing more noise to propagate beyond the barrier. This diffraction reduces the effectiveness of the barriers across different frequencies. Additionally, these designs block airflow and light to adjacent areas, which can negatively impact nearby residents. Therefore, it is crucial to develop novel types of barriers that can address these issues and effectively attenuate the constantly shifting dominant frequencies of traffic noise, thereby reducing the harmful effects of noise pollution.

In this study we developed an adaptive acoustic metamaterial by integrating phononic (or sonic) crystals with phase-transforming cellular materials (PXCMs)(Fig 3).  PXCMs are innovative materials that can be designed with a bistable configuration [8], allowing them to reconfigure the periodic arrangement of phononic crystals dynamically. Fig. 3 (c) and (d) presents a schematic of the structure featuring hexagonal lattice patterns in both open and closed configurations. This reconfigurability is essential because it enables the periodic structure of the phononic crystals to adapt to varying traffic noise frequencies, enhancing noise mitigation across a broad spectrum. 3DP cement paste sample with triangle configuration was used as the column elements in the phononic crystals. As illustrated in Figure 3, using PXCM as an actuator allows the arrangement of phononic crystals to be actively modified. The spacing between the columns of these crystals is a key factor that determines the specific frequencies at which noise is mitigated. Adjusting these distances can significantly adapt the spectral properties of the bandgaps, allowing the metamaterial to respond effectively to changes in noise frequency. Research by Thota et al. (2017) has demonstrated that compact hexagonal patterns are particularly effective at mitigating high-frequency noise compared to more loosely arranged hexagonal patterns. This finding underscores the potential of Reconfigurable acoustic metamaterials in applications where adaptive noise control is crucial, such as in urban environments affected by fluctuating traffic noise levels.

Fig. 3 - (a) Periodic pipe noise barrier on a highway [7]; (b) illustration of the phononic/sonic crystal noise barrier; (c) schematic and specimens developed for reconfigurable phononic/sonic crystals integrated with phase-transforming cellular materials (PXCMs), featuring hexagonal lattice patterns in two configurations: (c) open configuration and (d) closed configuration.

The barrier is planned to be positioned as depicted in figure 4 (a), further work in the lattice design will be accomplished to make the barrier a modular assembly, taking advantage of the modular nature of the proposed lattice.Since the horizontal movement of the barrier must be allowed, rolling supports will be used to support the barrier weight, while mechanical actuation can physically reconfigure the lattice arrangement, enabling adaptability in response to change noise frequencies. Reconfigurability in acoustic metamaterials can be achieved through several methods. Hydraulic systems can be employed to adjust the spacing or configuration of the phononic crystals by applying pressure to move structural elements. Mechanical actuation, such as the use of motors or springs, can physically reconfigure the lattice arrangement, enabling adaptability in response to change noise frequencies. Cable-based systems provide another method by pulling or tensioning specific components to alter their positions.

Fig. 4 - (a) Proposed periodic noise barrier with reconfigurable lattice: (b) Supports and forces to be applied to assure barrier reconfiguration.

Task 3: Material Characterization and Testing

Tasks 3.1: 100% complete

The reader is recommended to refer to the previous quarterly report for the results of quasi-static test. In the report we present the result for dynamic (drop-tower) impact tests to evaluate performance of the bio-inspired architectures under impact loading condition. Drop tower impact test was conducted for sample with 3DP and casted fiber reinforced mortar.  Five sample configuration was tested including: cast mortar with and without fiber, 3DP sample with bouligand, sinusoidal bouligand, and regular straight printing configuration (Fig. 5). The drop was conducted with two impact energy: 56.7J and 70.9J.

Fig. 5- (a)Schematic showing schematic of 3DP configurations with different architectures including Bouligand, Sinusoidal helicoidal and regular configuration

architecture under drop tower impact test (b) Instron drop tower used in this study

Fig 6 presents the load-deflection results and fracture patterns from the drop tower impact test for cast samples (with and without fiber) and 3D-printed samples using Bouligand, sinusoidal Bouligand, and regular straight filament configurations, subjected to impact energies of (a) 56.7J (drop height of 0.8m) and (b) 70.9J (drop height of 1m). The force-displacement curves highlight the differing abilities of these configurations to respond to dynamic impact loads and absorb energy. The higher peak loads and delayed decline in the curves for the sinusoidal Bouligand and Bouligand samples indicate their enhanced impact resistance at both energy levels. At a drop height of 0.8m(Fig. 6(a)), the sinusoidal Bouligand sample achieved the highest peak force (14,666.4N) and absorbed 56.6J of energy, while the Bouligand sample reached a peak force of 9,968.5N, absorbing 53.6J of energy. The sinusoidal Bouligand sample demonstrated the highest peak load of all samples and exhibited similar energy absorption to the Bouligand sample. The sinusoidal Bouligand design outperformed the other configurations, with a peak load 52.4% higher than the regular 3D-printed samples and 34.8% higher than the cast samples with fiber, while its absorbed impact energy increased by 20.8% and 29.7%, respectively. Compared to the cast sample without fiber, the sinusoidal Bouligand sample showed a 98.8% increase in peak load and a 102.6% increase in absorbed impact energy.

Fig. 6 - Load-deflection results and fracture patterns from the drop tower impact test for cast samples (with and without fiber) and 3D-printed samples with Bouligand, sinusoidal Bouligand, and regular straight filament configurations, subjected to impact energies of (a) 56.7J (drop height of 0.8m) and (b) 70.9J (drop height of 1m).

As shown in Fig. 6(b), At an increased impact energy of 70.9J (from a drop height of 1m), the sinusoidal Bouligand sample shows peak force of 14,133.8N and absorbed 66.3J of energy, while the Bouligand sample reached a peak force of 12,192.5N, absorbing 68.7J of energy. The cast sample with fibers exhibited a peak load of 8,383.8N and absorbed 44.5J of impact energy. The sinusoidal Bouligand and Bouligand samples surpassed the peak load of the cast sample by 68.6% and 45.4%, respectively, and exceeded its absorbed impact energy by 49.2% and 54.6%. Compared to the results at the drop height of 0.8m, the energy absorbed by the sinusoidal Bouligand and Bouligand samples increased, while the energy absorbed by the cast sample remained similar due to the fatal damage it sustained

Fig. 7 (a) compares the fracture patterns and Ashby plot, illustrating the average peak impact load and absorbed energy for different samples under an impact energy of 56.7J (drop height of 0.8m). It is evident that the sinusoidal Bouligand sample exhibits the highest peak load and absorbed energy compared to the other configurations. The Bouligand sample shows a slightly lower peak load but similar absorbed energy compared to the sinusoidal Bouligand. Notably, both the sinusoidal Bouligand and Bouligand samples outperform the cast samples. As seen in the fracture pattern images, these designs demonstrate excellent resistance to crack propagation and maintain their structural integrity. In contrast, the cast samples (with and without fiber) and the regular 3D-printed samples suffer significant structural damage, failing to absorb the full impact energy and and exhibiting severe failure. These results underscore the superior impact resistance of the sinusoidal Bouligand and Bouligand structures. Fig. 7 (b) compares the fracture patterns and Ashby plot, showing the average peak impact load and absorbed energy for different samples under two impact energy levels(56.7J and 70.9J). Both the sinusoidal Bouligand and Bouligand samples exhibit increased energy absorption as the imposed energy rises. These designs are more effective under impact loading conditions compared to the cast samples, owing to their ability to prevent fatal crack development and maintain structural integrity. In contrast, the cast samples fail to absorb higher impact energy due to the extensive

Fig. 7 – Results of drop tower impact test(a) Comparison of fracture patterns and Ashby plot showing the average peak impact load and absorbed energy for different samples under two impact energies: 56.7J (drop height of 0.8m) and 70.9J (drop height of 1m); (b) Comparison of peak impact load and absorbed energy for different samples under an impact energy of 56.7J (drop height of 0.8m)

damage they sustain under both conditions.

As mentioned in the project description section , as electric vehicles (EVs) become increasingly prevalent, traditional roadside barriers face significant challenges due to the greater impact forces these heavier vehicles generate. Current designs, optimized for lighter gasoline-powered vehicles, often fail to adequately contain EVs, leading to catastrophic failures during collisions that impact both the infrastructure and the vehicle [1]-[5]. Our research highlights the potential for innovative barrier designs that leverage advancements in materials and engineering, specifically through the use of bio-inspired architectures and 3D printing technology. The results from our dynamic impact tests indicate that the sinusoidal Bouligand and Bouligand configurations significantly enhance energy absorption and impact resistance, making them highly suitable for modern roadside barriers. These designs exhibit a remarkable ability to prevent fatal crack development while maintaining structural integrity, which is critical as the weight of the vehicle fleet continues to evolve. The enhanced energy dissipation capacity of these materials translates into improved deflection during impact, allowing barriers to effectively manage the forces exerted by heavy trucks. This capacity for deflection is particularly important, as it enables the barrier to absorb energy while reducing the velocity of the impacting vehicle. By dissipating energy effectively, these barriers not only minimize damage to themselves but also protect the vehicles involved, enhancing overall safety. This design approach is crucial for preventing heavy trucks from rebounding into traffic or penetrating the barrier, which could have catastrophic consequences for road users. In summary, our findings underscore the necessity of re-evaluating and redesigning roadside barriers in light of the evolving vehicle landscape. By incorporating bio-inspired designs and advanced materials, we can develop barriers that better withstand the challenges posed by modern vehicles, particularly heavier EVs, thereby significantly improving roadway safety.

Tasks 3.2: 100% completed(still working on this section)

The purpose of this experiment is to measure the noise absorption ratio of a barrier under two different shape configurations in a controlled environment with noise isolation. The barrier is a shape-shifting structure, and by changing its shape, the distance between the phononic crystals embedded in the barrier varies. The goal is to observe how this change in configuration affects the barrier’s ability to absorb sound at different frequencies. Specifically, we aim to determine how efficient the barrier is at absorbing noise in both configurations and how the absorption ratio shifts across the frequency spectrum.

Fig. 8 – Noise absorption experiment set up.

A MATLAB code was implemented to facilitate this experiment by generating sound at various frequencies (100 Hz to 2000 Hz), playing these frequencies through a speaker on one side of the barrier, and recording the sound on the other side using a microphone. The RMS power of the original signal is compared to that of the recorded signal, and the difference is used to calculate the noise absorption ratio, given by the formula:

Absortion Ratio=1-RMS of Original SignalRMS of Recorded Signal​​

By running the experiment in both barrier configurations, we can analyze the variation in the noise absorption ratio across different frequencies and identify which configuration provides more effective noise absorption at specific frequencies. The plot of absorption ratio vs. frequency will reveal how the phononic crystal arrangement impacts sound attenuation in each configuration.

(a)

(b)

(c)

Initially, the experiment was performed without the sound barrier in place. This was done to observe the system's behavior without the effect of the barrier. Figure 9 depicts the results under these conditions. Noticeable high peaks at 1400 Hz and 1800 Hz suggest that the system is resonating at these frequencies. Since this phenomenon is consistent each time the experiment is performed under these conditions, we can assume that the peaks are due to system resonance. Resonance at these frequencies may cause the sound waves to cancel each other out, which could explain why the program registers a higher noise absorption ratio at those points.

Fig. 9 Absorption Ratio – Frequency graphics, a, b and c show the results for the experiment without having placed the sound barrier inside the box. (repeated under the same condition)

Another behavior to be analyzed in the graph is the presence of values lower than zero. This occurs because noise from outside the box, combined with the source noise, causes the ratio RMS of Original SignalRMS of Recorded Signal​​  to be greater than one, resulting in negative absorption values.

Additionally, one more test was performed before placing the barrier inside the box. This time, the aim was to measure the noise absorption of the system without the speaker emitting any sound. This would reveal any significant variations in the absorption ratio across the frequency spectrum. Figure 10 shows the expected absorption ratio values (close to one), slightly influenced by external sound.

Fig. 10 Absorption Ratio – Frequency graphic (speaker not emitting sound).

Once the external disturbance was measured, we proceeded to place the barrier inside the box and ran the program for both barrier configurations. The results are depicted in Figure 11 (a) and Figure 11 (b).

(b)

(a)

Fig. 11 Absorption Ratio – Frequency graphics when a) Sound barrier set in its closed configuration b) Sound barrier set in its open configuration.

By comparing both graphs, it can be observed that the noise barrier had no significant impact in the open configuration, aside from slightly lowering the system's resonant frequency. In the closed configuration, the barrier showed a small effect, specifically at 1300 Hz.

Given these results, it was necessary to conduct a literature review to explore a scaling procedure used in previous studies. The work of M. Thota and K. W. Wang, Reconfigurable Origami Sonic Barriers with Tunable Bandgaps for Traffic Noise Mitigation [7], suggests that when scaling, higher frequencies are used for testing, proportional to the dimensional scaling of their prototype. Following this insight, the experiment was repeated with frequencies ranging from 2.5 kHz to 10.5 kHz with increasement intervals of 500 Hz. The results are depicted in Figures 12 and 13.

Fig. 12 Absorption Ratio – Frequency graphic showing the results for the experiment without having placed the sound barrier inside the box.

(a)

(b)

Fig. 13 Absorption Ratio – Frequency graphics when a) Sound barrier set in its closed configuration b) Sound barrier set in its open configuration, both performed at higher frequencies.

This time, variations in the results were noticeable with both the presence of the barrier and the change in its configuration. When opening the barrier, compared to the closed configuration, a change in the absorption ratio was observed at 4 kHz. Additionally, there was a slight shift in the frequency range where the barrier was mitigating noise, expanding from the 4000–4500 Hz range to the 4000–5000 Hz range. However, the absorption ratio in this extended range was nearly half the values observed with the closed configuration.

At 9000 Hz, in both the experiment without the barrier and with the barrier in the open configuration, a peak appeared, which suggests a resonance frequency in the system. Notably, this peak shifts to 10 kHz when the barrier is closed. Figure 13 (b) also shows a sudden increase in noise absorption at 10.5 kHz, which may be linked to the closed configuration's altered impact on sound attenuation. This increase could be explained by a shift in the system’s resonance due to the barrier’s geometry, which may introduce new resonant frequencies. Additionally, the barrier could be creating constructive interference or forming a bandgap at this frequency, both of which would result in enhanced sound absorption.

To confirm the behavior observed in the last results, the experiment was repeated this time modified to obtain more datapoints. Going from 100 Hz increases to 10 Hz increases in the 2500 to 10500 Hz range, the results are depicted in figure 14.

Fig. 14 Absorption Ratio – Frequency graphic for the experiments result for the box without the sound barrier.

Again, the experiment was performed without the barrier to observe the effect of system resonance and external noise in the noise absorption ratio. We can see that the peak observed at 4000Hz in figure 13 (a) and (b) is present again, which puts in consideration the assumption that the peak was introduced by the presence of the barrier and confirms the need of more data.

Fig. 15 Absorption Ratio – Frequency graphics for the experiments result for the sound barrier set in the open position inside the box.

Figure 15 shows 2 graphics corresponding to the experiment results when performed with the barrier in the open configuration, by observing the three graphics, we can notice that not only we are getting new data due to the data points increase, but also consistent results when performing the experiment under the same conditions. Now we can see how noise absorption peaks are now present along the frequency spectrum, which makes sense due to having positioned the barrier in the system. Now, we want to observe how those peaks change when changing the barrier configuration, both the frequency where the peak is and the peak absorption ratio value for the given frequency.

Figure 16 depicts the results for the experiment with the noise barrier set in the closed configuration, in the same way as in figure 14, the experiment was performed twice to confirm consistency.

Fig. 16 Absorption Ratio – Frequency graphics for the experiments result for the sound barrier set in the open position inside the box.

The most significant change in the frequency range occurred at 6140 Hz, where the absorption ratio went from 0.284 to 0.914, as well as in higher frequencies for frequencies above 10 kHz, the absorption ratios increased to almost double with respect to the ones obtained with the closed configuration.

In accordance with the scale factor previously described, which was chosen based on the literature [7], for real applications, we expect to have the major impacts in frequencies around 877.142 Hz and 1428.571 Hz and above.

These low-cost DIY experiments demonstrate the possibility of altering the barrier’s working frequency intervals, but also highlight the possibility to implement more complex data analysis and filtering methods to better understand and mitigate the effects of external noise and system geometry on the results. Further work will focus on increasing both noise absorption and stabilize the effect of the change in barrier configuration along the spectrum by modifying the shape-shifting lattice geometry, as well as incorporating other noise-mitigating metamaterials into the barrier.

- Percent of research project completed

100%

- Expected progress for next quarter

This phase one project is 100% completed.

- Educational outreach and workforce development

- During the summer of 2024 (06/2024-08/2024), the research team is collaborating with two Purdue Summer Undergraduate Research Fellows and industry partner Terran Robotics on projects focusing on sustainable earth-based materials and additive manufacturing technology. This research project enables students to explore the impact of novel materials and technologies on the development of general and transportation infrastructures.

- This summer, our lab had the pleasure of hosting two enthusiastic groups of undergraduate students from Purdue University's ‘Summer College for High School Students’ and the ‘Gifted Education Research and Resource Institute’. These students were eager to learn about 3D printing concrete, and they sought out our lab at Purdue University because of our leading-edge research in this area. We delivered a lecture covering the fundamentals of 3D printing technology. We provided an overview of various 3D printing systems, with a particular focus on their applications in cementitious materials. This lecture aimed to provide students with a understanding of the principles and innovations driving 3D printing technology. Students also participated in lab demonstrations focused on 3D printing concrete. The visit featured notable demonstrations using both a small-scale gantry system and a large-scale robotic arm system. The lab demonstrations highlighted the precision and versatility of the  3D printing equipment in creating intricate designs, and also showcased the technology’s ability to manage larger projects and its practical applications in real-world construction scenarios. Another part of the visit was dedicated to demonstrating the compressive testing of 3D printed samples. This test provided insight into the mechanical properties of the printed structures.  Additionally, we demonstrated the use of digital image correlation (DIC) to track strain and crack development in the 3D printed samples. This technique allowed students to observe how strain and crack propagation are monitored and analyzed in real time, adding a valuable dimension to their understanding of material performance. Throughout the visit, the students were actively engaged, asking insightful questions and displaying a keen interest in the advanced applications of 3D printing technology. The combination of lectures, hands-on demonstrations, and practical testing provided them with a comprehensive and engaging experience.

- Technology Transfer

Patent submitted under review:

- Youngblood, J. P., Olek, J., Zavattieri, P. D., Wang, Y., Douba, E. A., Low Carbon, Low Cost Cement Mix Containing Cellulose Nano Fiber and Limestone Filler For 3D Concrete Printing, under review

- Zavattieri, P. D., Youngblood, J. P., Olek, J., Wang, Y., Energy-Absorbing Roadside Barriers Using Bio-Inspired Architecture and 3D Concrete Printing

- Zavattieri, P. D., Youngblood, J. P., Olek, J., Wang, Y., Cubillos, L. David, Reconfigurable acoustic metamaterials for traffic noise reduction

- Zavattieri, P. D., Olek, J., Marika Santagata, Youngblood, J. P., Wang, Y., Hygrolock-reinforcement for building blocks made of earth materials

Research Contribution:

- Papers that include TRANS-IPIC UTC in the acknowledgments section:

Two papers under preparation, will include TRANS-IPIC UTC in the acknowledgments section:

•	Y. Wang, J. Olek, J. Youngblood, P. Zavattieri, Biomimetic Sinusoidal Helicoidal Architectures Enhance Strength and Impact Resistance of Additively Manufactured fiber reinforced cementitious composite.

•	Y. Wang, A. Douba, J. Olek, J. Youngblood, P. Zavattieri, Sustainable Cementitious Composite Containing Cellulose Nano Fiber and Limestone Filler for Concrete 3D-Printing.

- Presentations and Posters of TRANS-IPIC funded research:

- Present poster in Purdue Civil and Construction Engineering Research Showcase

- Please list any other events or activities that highlights the work of TRANS-IPIC occurring at your university (please include any pictures or figures you may have). Similarly, please list any references to TRANS-IPIC in the news or interviews from your research.

No to date

References:

[1] Nebraska tests suggest U.S. highways are not ready for widespread EV use | Nebraska Today (unl.edu)

[2] Nebraska experts weigh highway safety and electric vehicles | Nebraska Today (unl.edu)

[3] UNL researchers test roadside barriers against heavy EVs in new study | Nebraska Public Media

[4] UNL researchers test how electric vehicle crashes can damage road barriers (1011now.com)

[5] https://www.fischer.senate.gov/public/index.cfm/2024/7/solving-the-hidden-safety-risks-of-evs

[6]Fredianelli, L., Del Pizzo, L. G., & Licitra, G. (2019). Recent developments in sonic crystals as barriers for road traffic noise mitigation. Environments, 6(2), 14.

[7]Thota, M., & Wang, K. W. (2017). Reconfigurable origami sonic barriers with tunable bandgaps for traffic noise mitigation. Journal of Applied Physics, 122(15).

[8] Zhang, Y., Restrepo, D., Velay-Lizancos, M., Mankame, N. D., & Zavattieri, P. D. (2019). Energy dissipation in functionally two-dimensional phase transforming cellular materials. Scientific reports, 9(1), 12581.

[9] Yaraghi, N. A., Guarín‐Zapata, N., Grunenfelder, L. K., Hintsala, E., Bhowmick, S., Hiller, J. M., ... & Kisailus, D. (2016). A Sinusoidally Architected Helicoidal Biocomposite. Advanced Materials, 28(32), 6835-6844.